## Slide 1
Automated Hyperspectral Pyrometry of Bulk Crystal Growths
Naman Parikh1, Tyrel McQueen3,4,5,6, David Elbert2,3
1Carnegie Mellon University, 2Institute for Data Intensive Engineering and Sciences, 3Hopkins Extreme Materials Institute, 4JHU Department of Materials Science and Engineering, 5JHU Department of Chemistry, 6Institute for Quantum Matter

## Slide 2
How hot is this?

## Slide 3: Floating Zone Furnaces

## Slide 5
Control over the growth process
Relatively quick growths
Can be pressurized to create an isolated environment
Benefits

## Slide 6
Thermal Gradient
Heat transfer
Physics of the molten zone is largely unknown

## Slide 7: Modeling – NaNO3
Scott S. Dossa, Jeffrey J. Derby
https://doi.org/10.1016/j.jcrysgro.2022.126723
Notes: The temperature and thermal gradient throughout the molten zone is a fundamental parameter in how the growth happens and the resulting crystal
Takes temperature field as an initial input, models the fluid and heat flow
Is not connected to actual temperature data

## Slide 8: Nuetron Imaging – BaBrCl:5%Eu
Jeffrey J. Derby, et. al.
https://doi.org/10.1016/j.jcrysgro.2020.125572
Notes: This imaging is can track the liquid/solid interface but is not able to probe the thermal gradient or heat characteristics

## Slide 9: LDFZ Video
PARADIM Summer School 2022
https://data.paradim.org
Notes: There’s a lot of qualitative information here, but we have no quantitative measurement of temperature and the small variations throughout the molten zone

## Slide 10
Crystal Properties
Molten Zone Temperature
Notes: The temperature and the thermal distribution will affect the properties of the crystal we grow, but we don’t know exactly how. If we did, we could reverse engineer what we want the thermal distribution should look like during a growth. If we could have a live feed of the thermal distribution, we could compare what we have to what we want. From there we would want to know how to get what we want and how to make adjustments if needed

## Slide 11
Molten Zone Temperature
Materials Used:
Chemical Properties
Furnace Controls:
Rotation Speed
Pull Rate

## Slide 12
Molten Zone Temperature
Materials Used:
Chemical Properties
Furnace Controls:
Rotation Speed
Pull Rate
Crystal Properties
Notes: Once we have the knowledge going forward, we can go backwards, using temperature of the molten zone as a middleman to figure out how to get the crystal properties we want and use that information to make adjustments in real time
Here I need to explain why this model means that we need to be able to collect temperature data in real time

## Slide 13: Can all of this be automatic?
Notes: What do we need to make this happen?

## Slide 14: Research Question

## Slide 15: Research Question
How can we measure the temperature of an ongoing growth in real time?

## Slide 16: Hyperspectral Camera
Notes: Ours is not blue :(

## Slide 17: Hyperspectral
Traditional

## Slide 18: Why hyperspectral?
Notes: With more than 3 wavelengths, we can make interpolate the data into a blackbody radiation spectrum. The exact shape of a spectrum uniquely determines the temperature, so using some machine learning on this will get us temperature values for each pixel

## Slide 19: Part 1: Physical Mount

## Slide 23: The camera needs to move!

## Slide 24
Notes: Why does it need to move?
Important to note that the computer syncs the start of the image capture and the movement of the stage

## Slide 26
Notes: How do we make it scan?

## Slide 27
Notes: How do we sync the motor with the image capture? We are replacing the stage with the motor

## Slide 28: R-Pi mimics the stage
Signals from stage

## Slide 31
Detector
Notch Filter
Lens
Notes: Problem: Need to protect camera detector from stray laser light that could damage it

## Slide 32: Part 2: Temperature Analysis
Etekcity Infrared Thermometer Temperature Gun 774, Digital IR Temp Gun for Food, Cooking, BBQ, Pizza Oven, Reptile, Griddle Accessories, Non Contact Surface Outdoor Heat Gun

## Slide 33: Molten zone is a black-body
5500 K
Notes: The shape of the black-body spectrum is unique to the temperature (for example, the wavelength of the peak), so we can determine temperature using the spectrum measured by the camera

## Slide 34
Notes: Wavelength will be the independent variable, epsilon is emissivity

## Slide 37: Heated Carbon Rod Testing
3000 K
Notes: The shape of the black-body spectrum is unique to the temperature (for example, the wavelength of the peak), so we can determine temperature using the spectrum measured by the camera
Explain thoroughly what’s happening in the graph

## Slide 40: Heated Carbon Rod Testing
Notes: The shape of the black-body spectrum is unique to the temperature (for example, the wavelength of the peak), so we can determine temperature using the spectrum measured by the camera
Explain why this gives is better than before

## Slide 41: Part 3: Automate Everything

## Slide 43
Notes: Animate in one piece at a time

## Slide 45: So, how hot was it?

## Slide 46
Kelvin
So, how hot was it?

## Slide 47: Now the science begins…

## Slide 48
Probe fundamental floating zone growth physics
Understand heat flow within the molten zone
Design growths for desired crystal properties
Adjust growths in real time
Now the science begins…

## Slide 49
David
Tyrel
Evan Crites - help with using lab equipment, building the mount
Maggie Eminizer - OpenMSIStream and helping design the streaming pipeline
NSF - PARADIM #2039380 and VariMat Award 2129051
Acknowledgements

## Slide 50
Kelvin
So, how hot was it?