## Slide 1
Automated Hyperspectral Pyrometry of Floating Zone Growths
Naman Parikh1, David Elbert2, Tyrel McQueen3
1Department of Physics, Carnegie Mellon University
2Hopkins Extreme Materials Institute
3Department of Chemistry, Johns Hopkins University

## Slide 2
Digital Twins
“Set of virtual information constructs that mimics the … system”
“Has a predictive capability”
“Dynamically updated with data from it’s physical twin”
National Academies of Sciences, Engineering, and Medicine
https://doi.org/10.17226/26894
Notes: Firstly, we have a set of virtual constructs that mimic the system, which is what the simulation is. It has some predictive capability in returning temperature distribution and fluid flows, but it isn’t at the point of predicting the effects of the furnace controls or the crystal structure and properties. These models are built only on physics theory, but that isn’t enough for those other 2 parts. For that, the model needs to update and improve based on experimental data from physical growths. The models simulate temperature distributions, so what we want to do is collect some temperature distribution data from experiments to inform and validate the models.

## Slide 3
Scott S. Dossa, Jeffrey J. Derby
https://doi.org/10.1016/j.jcrysgro.2022.126723
Notes: What is a digital twin? It can take a lot of forms but generally it’s the idea of having a digital representation of some physical object or process. In our case, the physical twin includes the furnace growths, the materials, and the controls of the furnace like the rotation speed and pull rate of the rods. The digital twin is some manner of computational model that simulates the growth happening within the furnace. We would want this model to be able to simulate the evolution of the growth over time, how the growth reacts to changes to the furnace controls, and the crystal structure and properties resulting from the growth. So, let’s talk about the current state of the digital models and what we can do to improve them.

## Slide 4
Laser Diode Floating Zone
Notes: I worked on studying floating zone growths using the Laser Diode Floating Zone furnace that we have. Before I talk about what I did, I’ll give you a brief overview of how floating zone growths work.

## Slide 5
Scott S. Dossa, Jeffrey J. Derby
https://doi.org/10.1016/j.jcrysgro.2022.126723
Notes: We start with two rods mounted in the furnace vertically pointing at each other. The bottom rod is the crystalline rod while the top is the feed rod. Some source of heat points towards the center, melting the tips of the rods to create a liquid floating zone. The rods are then pulled apart and a crystal grows out of the liquid zone.

## Slide 6
Notes: This particular furnace uses lasers to heat the rods, and there are 5 set around the center. So, how can we go about studying how floating zone growths work and how to design growths? One big picture approach to think about is to think about the development of a digital twin for floating zone growths.

## Slide 7
Research Question
How can we collect temperature distributions across the molten zone?

## Slide 8
Hyperspectral Camera
Notes: With a hyperspectral camera, we can measure a full emission spectrum for each pixel. From there, we’ll have to do some analysis to figure out how to get temperature.

## Slide 9
Collect hyperspectral data from the molten zone
Process hyperspectral images into temperature distributions
Create a streaming process for real-time data
Notes: So, first and foremost is to get the camera set up in the furnace to be able to collect data. You can see the camera mounted there alongside the laser. Another detail is that the camera captures a line rather than a 2-D image, so it needs to scan up and down to capture a full image. The next thing is to analyze the data, but before I get into the details of how to do that, I want to talk about how exactly we set it up. We want to be able to collect a lot of data, so we want to be more efficient than manually capturing and analyzing each individual image separately. We also want the models to ultimately update automatically as new data comes in, so we should start laying the groundwork for that automation now. So, here’s how we do that.

## Slide 10
Pyrometry
Blackbody
Notes: Define pyrometry
So, how do we actually get temperature from hyperspectral data? The key observation is that a hot glowing material is a blackbody, and blackbody spectra are completely unique depending on the temperature of the object. It will be a little challenging because the camera only captures a limited range, but we’ll see how it goes.

## Slide 11
Blackbody Model Function
Emissivity
Parameters
Stray Light Offset
Notes: There’s 3 parts here. The middle is the actual core of the blackbody shape that should look familiar. The piece in front is an approximation of emissivity. Emissivity changes depending on the materials we use and can also vary over wavelength, so we use a quadratic expansion to model that dependence. Finally, there’s a constant offset at the end. This term improves the regression by adding some flexibility. Like any spectrum, blackbody radiation always goes to 0 as the wavelength goes to 0. However, forcing the fitting to stick to this turns out to cause some aggressive overfitting. The spectrum could be shifted up by stray light in the background or mistakes in correcting the spectrum against black and white references, so it helps to add this term to account for those things. With these added pieces, we have added parameters to optimize during the regression alongside temperature.

## Slide 12
Data
Fitted with T=1298 K
Full Spectrum
Notes: So, let’s take a look at how this works. Here’s a spectrum that we measured during testing. You’ll notice that it doesn’t quite look like a blackbody spectrum, and that’s because of the limited wavelength range that I mentioned. Nevertheless, if we run the regression, we get a nice looking fit and a reasonable temperature value of about 1000 C. We can also zoom out to see that we actually have been looking at a very small part of the blackbody spectrum, but the regression is still successful.

## Slide 13
Notes: We use something called data streaming. When the image is captured by the camera, it is automatically streamed out to a server. From there, the data is consumed by a stream processor that’s hosted on one of our paradim servers. There, the raw data is both stored in a database and also analyzed. The resulting temperature distribution is then streamed back out to the third party and then back to the lab so that the people doing the growth can see the results in real time.

## Slide 14
Into the furnace
14
Kelvin
Notes: So, taking this analysis into the furnace, here we have an image from a growth. There’s not much to see in the png because this growth was too dark to see much. We can fix that by increasing the exposure time, but it turns out that we are still able to get temperature well with a low exposure, so I stuck with that. Also, because we set up all the automation, this is super easy to run. I clicked capture image, waited, and got back this heatmap. **Talk about what this is looking at, what we see**

## Slide 15
Physical
Digital
Data
Measurement
Model validation and updating
Predictions
Promising growths
Notes: Finally, I want to take a step back and talk about how this fits into the bigger picture that I talked about at the beginning. This data is measured from physical experiments, and it can now be used to inform and validate the digital models that we talked about. Going the other way, we now speak a common data language so we can take the predictions the models dive and use them to inform future growths. Those growths in turn create more data, and the cycle of experimentation and improvement continues.

## Slide 16
Evan Crites (McQueen Lab, PARADIM)
Maggie Eminizer (IDIES)
NSF Awards #2039380 (PARADIM) and #2129051 (VariMat)
Acknowledgements
Physical
Digital
Data

## Slide 17
Least Squares Regression
Model Function
Parameters
Guess Parameters
Minimize Residuals
Notes: To do this, we can use least squares regression. With this regression method, we start by providing a model function, which we know for blackbody radiation. The regression than optimizes parameters of the function, which will include temperature that we want. We then guess some parameters, getting a bad fit, but the residuals are minimized and parameters optimized to get the best fit. There’s lots of code already written to do the last part, so what we need to do for this specific usage is figure out what the model function should be.

## Slide 18
Physical
Digital
Data
“Dynamically updated with data from it’s physical twin”
“Bidirectional interaction”
“Informs decisions that provide value”
Notes: This hits on the last

## Slide 19
Physical
Digital
Data
Autonomous Experimentation

## Slide 20
Extra Slides – Other Carbon Rod Spectra

## Slide 21
Overfitted
21

## Slide 22
Carbon Rod Corrected

## Slide 23
Carbon Rod Uncorrected

## Slide 24
Notch Filter Dip

## Slide 25
Laser Light Spike

## Slide 26
Extra Slides – Camera Motion

## Slide 27
Notes: How do we make it scan?

## Slide 28
Notes: Why does it need to move?
Important to note that the computer syncs the start of the image capture and the movement of the stage

## Slide 30
Notes: How do we sync the motor with the image capture? We are replacing the stage with the motor

## Slide 31
Extra Slides – Streaming

## Slide 33
Notes: Animate in one piece at a time